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	Product information
	An adhesion-promoting primer/sizer for non-porous surfaces.

· Dries with a permanent tack
· Water resistant
· Low odor, no spatter
· High yield 
· Non-flammable
· Penetrates up to 3 cm into the substrate, consolidating the surface
· Very Low V.O.C. (Volatile Organic Compounds)

	Recommended uses
	Recommended for application over non-porous or sealed surfaces. Its white color makes wall paints easier to apply.

	Coverage
	[bookmark: _Hlk102401543]Approximately 107 square feet per quart, depending on the porosity of the substrate.

	Application instructions
	[bookmark: _Hlk102554440]Surface preparation
Surface must be free from grease and all residues, dry, smooth and structurally sound. Repair all unsound surfaces. Clean ceramic tile, paneling, glass and sealed surfaces with isopropyl alcohol. For best results, lightly sand or abrade all glossy or sealed surfaces before applying. Before proceeding with any unusual conditions, consult your adhesive or wallcovering supplier. After the required surface preparation is completed, it is critical to test the surface to ensure compatibility. Select a small, inconspicuous area of the surface for testing and apply the primer or adhesive as specified. Inspect the test area after 24 hours before proceeding with the installation of wallcovering.

Product preparation
The product is ready to use. 
The product provides high coverage.

Application
Use only when room temperature is above 60°F (16°C).
Apply at the recommended spread rate using a roller or spray system.






Cleaning
Before the primer dries, remove any excess with clean water. Brushes and rollers should be cleaned immediately after use with a mild soap and clean, warm water.



	Technical product data

	Base
	Acrylic water-based

	
	Appearance and color 
	White liquid

	
	pH
	6.5-7.0

	
	Viscosity
	5000 cps 

	
	VOC
	<2 µg/m3

	
	Solids percentage
	50%

	
	Customs code 
	3209 1000

	
	Application temperature
	+41°F- +104°F (+5°C-+40°C)

	
	Drying Time
	3/4 hours

	
	Non-Flammable product
	

	
	Protect from frost
	

	Warning
	Do not apply to porous surfaces. Not recommended for direct application over oil-based primers. Protect from frost

	Storage

	The product is guaranteed in its original packaging, in standard conditions +41°F- +95°F (+5 °C to + 35 °C), for 24 months from date of production. It is important to keep the product in dry conditions, away from heat sources and direct sunlight.

	[bookmark: _Hlk102401875]Disclaimer

	If you scrape, sand, or remove old paint, you may release lead dust. Keep out of reach of children. Dispose of leftovers in special containers for building materials. The information contained in this data sheet is the result of our many years of experience but is only indicative. Therefore, those who want to use it are obliged to assess whether the product is suitable for use and take responsibility for its use. 
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PREPARATION DE LA SURFACE

La surface doit étre séche, lisse, solide et
propre. Vérifier la peinture, le papier peint
existant et les zones endommagées. Ré-
e les parties instables avan appica-

APPLICATION DU PRODUIT

Utiiser Primer STO-SP entre 65°F et 80°F
(18°C-25°C). Méanger avant usage. Appi-
qQuer une couche uniforme au pinceal, au
rouleau ou au pistoke.

NETTOVAGE

Nettoyer les outls & Feau immédiatement
aprés utlsation.
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